Silicone Softener DT-6258

Softener DT-6258 is a High-efficiency softener with good wash fastness for woven and  knitted fabrics made of cellulosics, synthetics and blends of these fibres, can be applied by padding or exhaust processes.

[Properties]

- Appearance: transparent liquid

- Chemical character: quat functional silicone copolymer

- Ionicity: weak cationic

- PH value: 6-6.5

- Solubility: soluble in water

- Storage: Can be stored for one year when the product is enclosed in the proper container under the room temperature.

[Features]

- Imparts a soft , pleasant , smooth handle to textile substrates.

- Improves the crease recovery angle and wash and wear behavior in combination with crosslinking agents for cellulosic fibres.

- No yellowing of white goods, which are treated with fluorescent brighteners.

- Application in the weakly acid condition ,but stable over a wide PH range.(tested to PH 2-12)

[Applications]

DT-6258 is easy to dilute by water in any ratio, it can be used directly.

Examples of use

Woven fabric handle  finishing

10-20g/l   DT-6258

pad, dry  at 120℃

Woven fabric resin finishing

60g/l  NFD

18g/l  CS-200

20g/l  DT-6500

15g/l  DT-6258

pad, dry and cure at 150℃ for 3 minutes.

[Packaging]

Packed in Plastic Drums and 125kgs Net Each.

The information and recommendations presented here were compiled with the utmost care,but cannot be extended to cover every possible case.They are intended to serve as non-binding guidelines and must be adapted to the prevailing conditions.